## Slide 1: Coal Refuse Materials–Common Mistakes and Misconceptions
BY: Gary Brill, PE

## Slide 2: Outline of Presentation
Coarse Refuse Placement, Compaction and Testing
Fine Refuse Placement and Testing

## Slide 3
A Little Perspective . . .
Coarse Refuse for Slurry Impoundment embankments is placed in maximum 12 inch thick lifts at a narrow range of moisture content to 95%
These Strict requirements are intended to take the guess work out of bulk fill construction
Should provide a simple and reliable system for the coal operator

## Slide 4
Besides . . .
Coarse Refuse properties are well documented and understood
Coarse Refuse makes an excellent embankment construction material
Out of plant moistures are typically close to optimum placement moisture
Coarse Refuse can be successfully placed year round
Until about 1992 Coarse Refuse was placed in 24 inch thick lifts and 90% compaction

## Slide 13
Misconceptions
Over-compaction results in a higher friction angle
Over-compaction results in a better material permeability
Over-compaction makes the dam safer

## Slide 14
95% of What? Let’s Go to the Lab

## Slide 21
ASTM D4718 Correction for Oversize Particles
May not be applicable to soil-rock mixtures which degrade under field compaction
Application above 30% may affect the unit weight
Document cannot replace experience and should be used with Professional Judgment

## Slide 23
Slurry
Oversize Correction for 12% retained on ¾ inch screen

## Slide 24
Oversize Correction for 30% retained on ¾ inch screen

## Slide 25
Where do you obtain your proctor sample?

## Slide 26
Corrected Max. Dry density = 132.8 pcf, Wcorr = 4.9 %
Corrected Max. Dry density = 132.5 pcf, Wcorr = 6.7 %

## Slide 27
Trained Eye of the Field Guy
Visual Observations from an experienced field technician are as important as confirmation field testing and paperwork

## Slide 29
Develop a Family of Curves to Cover Variations in the site specific Coarse Refuse materials
Each time field compaction tests are performed, also perform a one-point proctor test and select the most applicable curve
Continue to perform periodic Proctor Tests

## Slide 31
Perform a field moisture content for one-point proctor test and to correlate to nuclear density gauge readings

## Slide 32
Optimum moisture = 14.7 %, with no distinct curve
Use fresh coarse refuse for each compaction point (i.e., do not reuse refuse)

## Slide 33
Standard Proctor Max. Dry density = 119.7 pcf, Wopt = 8.7 %
Perform Oversize Correction
Corrected Max. Dry density
= 129.9 pcf, Wcorr = 6.8 %
Results yield about 96% to 97% compaction
Corrected results still yield 104 % compaction
Need New Proctor Test

## Slide 36
Develop Uniform beach of fine refuse along upstream embankment face
Dewater Pond as much as practical

## Slide 37
Start Upstream construction at dam abutment hugging upstream slope

## Slide 38
Start Upstream construction as early as possible and don’t get in a rush

## Slide 39
How much load can fine refuse bear?

## Slide 40
Clay-like versus Sand-like Fine Refuse for Seismic Strength Allowance – you can assume more for Clay
Plasticity Index PI is greater than or equal to 7
Plasticity Index = Liquid Limit – Plastic Limit
Problem is that Fine Refuse often has a PI of 5 or 6 but exhibits Clay-like behavior

## Slide 42
ASTM recommends at least 3 points – we recommend at least 5

## Slide 46
Triaxial Strain Behavior – if stress-strain curve shows no distinct drop off, then the material behaves as a Clay

## Slide 47
Coefficient of Consolidation If Cv < 3.3 ft2/day then materials behaves as a Clay

## Slide 48
Unconfined Compression Testing – Indication of Clay-like behavior?

## Slide 49
Summary
Use one-point proctors in the field for Coarse Refuse placement
Use engineering judgment when applying the oversize correction and assessing compaction of Coarse Refuse materials
Develop a uniform beach of Fine Refuse for seepage control and upstream construction
Most Fine Refuse is Clay-like and should be modelled accordingly